DESCRIPTION OF PROGRAM

This beamtime request is to support research funded by the NSF under the program title “Circularly polarized x-ray studies of ultrathin magnetic films.” This description is identical to last year’s since we are continuing all of the projects—they are longer term studies and have extended beyond one year’s allocation.

### Magnetic surface alloys: Mn/Ni(001), Mn/Co(001), etc.

The c(2x2) MnNi system is one of the many examples of epitaxial materials for which the elemental specificity of XAFS/XMCD is essential to understanding the magnetism. With this specificity, it is straightforward  to separate out the magnetic contributions of the two sublattices (Mn and Ni), which must otherwise be done indirectly.

There are a number of issues that we wish to pursue in the study of the MnNi surface alloy. To see what is so interesting, we first briefly summarize some of the properties of the bulk material. Bulk MnNi is antiferromagnetic (TN=800C), having a face-centered tetragonal (fct) structure, with the (002) a-b planes normal to the c-axis occupied alternately by all Ni or all Mn atoms. Within each a-b plane, consisting of a single element, the atoms are antiferromagnetically aligned, with the spins parallel to the plane (perpendicular to the c-axis).

The surface alloy is very different. Our circular dichroism results show that the c(2x2) MnNi surface alloy has ferromagnetic alignment of the Mn sublattice, and that furthermore the Mn-Ni coupling is also ferromagnetically aligned. This seems to support the argument that these systems, grown epitaxially on single crystal substrates, should be considered independent magnetic materials in their own right.

These results for the c(2x2) MnNi surface alloy are really remarkable, when the properties of the bulk MnNi alloy are considered, as determined by neutron scattering. Bulk alloys are anti-ferromagnetic, and the neutron scattering results have been interpreted as showing that the magnetic moment on the Ni atom is zero, for Mn content above 30%. We can grow stable films of MnNi up to about 8 ML in thickness, and all of these films show FM coupling of the Mn atoms, and a strong FM Ni moment. There is no chance of ambiguity in the interpretation of the XMCD results, since the signals are very large, and the interpretation is straightforward. The neutron scattering results, however, are very subtle to interpret, and there has been some long-standing disagreements and re-interpretations of the data over the last decade. Private communications with one expert in the field (Cable), convince us that the neutron result has ‘converged’ to agreement that the bulk alloy MnNi is anti-ferromagnetic, but that the precise moment on the Mn and Ni sites is still uncertain. We have no doubt that the surface alloy is a different magnetic structure, one that remains to be explained theoretically. We plan further measurements on thicker films, to see if there is need to reopen the question of the magnetic structure of the bulk alloy.

We are also investigating Mn/Co structures, which are closely related[]. Very similar variances between neutron results for bulk alloys, and our results for surface alloys, are found in this system as well. In particular, the literature on dilute Mn alloys with Co is very controversial: the neutron results say that Mn-Co is an antiferromagnet (AF), while NMR results claimed that it was ferromagnetic (FM). The ‘final word’ was had by neutron scattering, claiming AF alignment of the Mn and Co moments. Our XMCD measurements see the opposite—we find FM ordering of the Mn and Co moments. It is impossible to get this wrong with XMCD, because of the element specificity and the direct measurement of the sign of the coupling. We are being very careful with these measurements. If we are right, then neutrons got the whole magnetic phase diagram of Mn binary alloys wrong, NMR was ambiguous, and X-ray scattering was useless (these aren’t ordered alloys). If we are right, we will have direct evidence for why circularly polarized synchrotron radiation is essential, indispensible, irreplaceable, and unique for magnetic measurements

Fig. 1 : Spin orientation reversal induced in fcc Mn/Co(001) by oxidation.

### Chemically induced magnetization reversal

This is an intriguing new direction for our research, which directly follows on the study of the sign of the coupling of magnetic overlayers to ferromagnetic substrates. We have found that the sign of the coupling of Mn to Fe and Co is not what has been predicted theoretically. If we use the d-band hybridization concept as a guide[], it suggests that ‘doping’ the Mn layer to reduce the electron concentration might alter the coupling to the substrate. This idea motivated us to examine Mn/Co(001) films exposed to oxygen.

The results were quite surprising. Only a small exposure to oxygen (3L) results in a complete reversal of the coupling of Mn to the Co substrate, from ferromagnetic to anti-ferromagnetic. The magnitude of the Mn spin moment remains the same. At the same time, the easy axis of magnetization rotates in the plane by 90o. The ease with which this spin reversal can be observed is seen in Fig. 1, where the independent spin moment of Mn and Co are shown through XMCD.

Fig. 2: Element-specific XMCD hysteresis loops of Co, in 1 ML Mn/Co(001). (a) as grown, FM coupling, (b)after exposure to oxygen, AF coupling.

These are very interesting observations, and we are proposing to follow up with a number of new investigations on this system. We point out some of the reasons why these new observations are interesting.

It is apparent that the Mn oxidizes to some extent during the exposure, which forms a chemisorbed layer that is disordered (no new LEED pattern appears). However, the film is still metallic (as indicated by the Fermi level). Also, the Mn atoms are ferromagnetically aligned within the Mn plane—this plane itself is anti-ferromagnetically coupled to the substrate. It is important to understand this distinction. Manganese oxide is an antiferromagnet, in which super-exchange through oxygen atoms makes the direction of the Mn spin flip from Mn site to Mn site. Nothing of the sort is happening in the present case.

There have been scattered reports of other unusual magnetic changes that result from exposure to very small amounts of adsorbate atoms, including a spin rotation in the plane of Co/Cu(100) that is very reminiscent of what we have found for Mn/Co(001)[,]. We believe there is a close relationship between the adsorbate induced easy-axis rotation, and that found on stepped substrates as a function of film thickness[], and that it clearly is related to changes in film strain, step-atom anisotropy, and dislocation density[].

We would like to point out that the observation of a spin reorientation due to chemical modification suggests a highly sensitive and interesting new type of chemical sensor. This chemical sensor would consist of a chemically active layer, Mn in this case, strongly coupled to a fixed magnetic layer, Co in this case. This sensor layer would then in turn be part of a spin-valve structure. When the Mn layer is exposed to small amounts of the target gas (oxygen), the net magnetic moment of the Mn-Co bilayer changes (by a large amount), changing the magnetoresistance of the spin valve. The surface, element specific, XMCD hysteresis loops of the Mn/Co(001) are shown before and after exposure to oxygen in Fig. 2. The change in total moment of the system is the sum of the two loops, which add in (a), before oxidation, and largely cancel in (b), after oxidation.

Fig. 3: Sharp transition in coercive field of a metastable bcc Ni(001) film occurs at the critical layer thickness for misfit dislocation formation. The transition is much sharper than the strain relief curve.

### Morphology and Magnetism

Interest in ultrathin film magnetism is turning towards some very subtle and fascinating effects: the interplay between film morphology (at the nanoscale) and magnetic properties. We are directing our efforts to look at the effects of strain relaxation and steps on element-specific hysteresis loops, net magnetization, coercivity, and magnetic anisotropy. That very small structural changes cause tremendous magnetic effects can be seen everywhere in the field. For example, the addition of one monolayer of Fe to the Fe/Co(001) system, at the right thickness, causes a transition from ferromagnetism to anti-ferromagnetism in the Fe layers (with the exception of the Fe/Co interface iron atoms)[,].

We have recently completed an initial study of the change in coercive fields (magnetic hardness) for ultrathin films of Ni, Co, and Fe, as a function of the film thickness, using XMCD as a quantitative probe of film magnetization. What we find is that there is an onset of a transition in coercive field in these films at the critical thickness of epitaxial growth, that is, at the onset of the formation of misfit dislocations (see Fig. 3). The shape of the transition in coercivity was much sharper than the rate of injection of misfit dislocations, an effect which we were the first to report[].

In later work, this effect was explored by simultaneously measuring the film lattice constant by RHEED, so that a direct comparison can be made of the shape of the lattice strain relief curve and the change in coercivity[Error: Reference source not found]. Our observation that the coercivity change is sharp compared to the strain relief was confirmed.

REFERENCES FOR PROGRAM DESCRIPTION

PUBLICATIONS OF WORK DONE AT SRC (1995-97)

- “Magnetic properties of Mn/Cu and Mn/Ni c(2x2) surface alloys,” W. L. O'Brien and B. P. Tonner, Phys. Rev. B 51, 617 (1995).

- “X-ray magnetic circular dichroism study of Fe-V multilayers,” G. R. Harp, S. S. P. Parkin,. W.L. O’Brien and B. P. Tonner, Phys. Rev. B (Rap. Comm.) 51, 3293 (1995).

- “Magnetic and structural properties of ultrathin Mn and Fe films on Ir(111),” W. L. O'Brien and B. P. Tonner, J. Vac. Sci. Technol. A 13, 1544 (1995).

- “Application of photoelectron spectromicroscopy to a systematic study of toxic and natural elements in neurons,” G. De Stasio, D. Dunham, B. P. Tonner, D. Mercanti, M. T. Ciotti, P. Perfetti and G. Margaritondo, J. Synchrotron Rad. 2, 106-112 (1995).

- “Induced Rh magnetic moments in Fe-Rh and Co-Rh alloys using x-ray magnetic circular dichroism,” G. R. Harp, S. S. P. Parkin, W. L. O’Brien and B. P. Tonner, Phys. Rev. B (Rap. Comm.) 51, 12037 (1995).

- “Synchrotron radiation photoelectron emission microscopy of chemical vapor deposited diamond electron emitters,” J. D. Shovlin, M. E. Kordesch, D. Dunham, B. P. Tonner and W. Engel, J. Vac. Sci. Technol. A 13 (1111) 1995.

- “Magnetic phases of ultrathin Fe films on fcc Co(001),” W. L. O’Brien and B. P. Tonner, Surface Science 334, 10-18 (1995).

- “Development of Electron Spectromicroscopy,” B. P. Tonner, D. Dunham, T. Droubay, J. Kikuma, J. Denlinger, E. Rotenberg and A. Warwick, J. Elec. Spectrosc. and Rel. Phenom. 75, 309-332 (1995).

- “Room temperature magnetic phases of Fe on fcc Co(001) and Ni(001),” W. L. O’Brien and B. P. Tonner, Phys. Rev. B 52, 15332 (1995).

- “Effects of ferromagnetic capping layers on the perpendicular anisotropy of Ni/Cu(001) films,” W.L. O'Brien and B.P. Tonner, Applications of Synchrotron Radiation Techniques to Materials Science, Materials Research Society Symposium Proceedings Vol. 375, 77-80 (1995).

- “Laterally resolved measurements of cesium iodide quantum yield,” T. dell’Orto, J. Almeida and B. P. Tonner, J. Vac. Sci. Technol. A 13, 2787 (1995).

- “Microanalysis surface studies and photoemission properties of CsI photocathodes,” J. Almeida, A. Braem and B. P. Tonner, Nuclear Instruments Meth. Phys. Res. 367, 337 (1995).

- “An electron imaging approach to soft x-ray transmission spectromicroscopy,” G. De Stasio, G. F. Lorusso, T. Droubay, M. Kohli, P. Muralt, P. Perfetti, G. Margaritondo, T. F. Kelly, and B. P. Tonner, Rev. Sci. Instrum. 67, 737-741 (1996).

- “New magnetic phases of Fe on fcc Co(001) and Ni(001),” W. L. O’Brien and B. P. Tonner,  J. Appl. Phys. 79, 5629-5631 (1996).

- “Anomalous perpendicular magnetism in Ni/Cu(001) films and the effects of capping layers,” W. L. O’Brien and B. P. Tonner, J. Appl. Phys. 79, 5623-5625 (1996).

- “Zinc uptake by brain cells: surface versus bulk,” G. De Stasio, S. Pochon, G. F. Lorusso, B . P. Tonner, D. Mercanti, M. T. Ciotti, N. Oddo, P. Galli, P. Perfetti, and G. Margaritondo, J. Phys. D: Appl. Phys. 29, 2209-2215 (1996).

- “Photon energy dependence of valence band photoemission and resonant photoemission of polystyrene,” J.Kikuma and B.P.Tonner, J. Electron Spectrosc. Rel. Phenom. 82, 41-52 (1996).

- “XANES spectra of a variety of widely used organic polymers  at the C K-edge,” J.Kikuma and B.P.Tonner, J. Electron Spectrosc. Rel. Phenom 82, 53-60 (1996).

- “Transitions in the direction of magnetism in Ni/Cu(001) ultrathin films and the effects of capping layers,” W.L. O’Brien, T. Droubay and B. P. Tonner, Phys. Rev. B 54, 9297 (1996).

- “A photoemission microscope with a hemispherical capacitor energy filter,” B. P. Tonner, D. Dunham, and T. Droubay, J. Elec. Spectrosc. Rel. Phenom. 84 (1997), 211-229.

- “Magnetic ordering in submonolayer Mn films on fcc Co(001), and the effects of oxidation,” W. L. O’Brien and B. P. Tonner, submitted to Phys. Rev. B.

VITA (One page only)

Brian P. Tonner

EDUCATION:

Cornell University, Ithaca, NY, Post doctoral fellow (1983)

University of Pennsylvania, Philadelphia, PA, Ph.D. Physics (1982)

University of Pennsylvania, Philadelphia, PA, M.Sc. (1978)

Brown University, Providence, RI, B.Sc. (1976)

CURRENT POSITION:

Director, Laboratory for Surface Studies

University of Wisconsin-Milwaukee

PAST EMPLOYMENT:

Senior Scientist (visiting) 1996-97

Lawrence Berkeley National Laboratory,  sabbatical leave from UW-M.

Associate Director, 6/91-8/95.

Synchrotron Radiation Center, University of Wisconsin-Madison.

Professor, 6/92-present.

Dept. of Physics, University of Wisconsin-Milwaukee.

Associate Professor, 6/88-6/92.

Dept. of Physics, University of Wisconsin-Milwaukee.

Assistant Professor, 9/83-6/88.

Dept. of Physics, University of Wisconsin-Milwaukee.

Research Fellow, 6/82-9/83.

Physics Department, Cornell University, Ithaca, NY

PROFESSIONAL RECOGNITION:

Co-founder, Surface and Interface Magnetism Group, American Vacuum Society, 1996.

Chair of AVS Surface Science Division Executive Committee, 1995-96.

Award for Excellence in Research, UWM Graduate School, 1994.

Post-doctoral Research Fellowship from IBM-Watson Research Center, 1982.

American Vacuum Society Scholarship, 1981.

University Fellow, University of Pennsylvania, 1980-1982.

Honors in Physics, Brown University, 1976.

“Spin reversal in Mn films induced by oxidation,” W. L. O’Brien and B. P. Tonner, submitted to JVST.

S. Mirbt, O. Eriksson, B. Johannson, and H. L. Skriver, “Magnetic coupling in 3d transition-metal monolayers and bilayers on bcc(100) iron,” Phys. Rev. B 52, 15070 (1995).

W. Weber, C. H. Back, U. Ramsperger, A. Vaterlaus, and R. Allenspach, “Submonolayers of adsorbates on stepped Co/Cu(100): switching of the easy axis,” Phys. Rev. B 52, R14400 (1995).

M. E. Buckley, F. O. Schumann and J. A. C. Bland, “Strong changes in the magnetic properties of ultrathin Co/Cu(001) films due to submonolayer quantities of a nonmagnetic overlayer,” Phys. Rev. B 52, 6596 (1995).

W. Weber, A. Bischof, R. Allenspach, C. H. Back, J. Fassbender, U. May, B. Schirmer, R. M. Jungblut, G. Guntherodt, and B. Hillebrands, “Structural relaxation and magnetic anisotropy in Co/Cu(001) films,” Phys. Rev. B 54, 4075 (1996).

U. Ramsperger, A. Vaterlaus, P. Pfaffli, U. Maier and D. Pescia, Phys. Rev. B 53, 8001 (1996).

“Magnetic phases of ultrathin Fe films on fcc Co(001),” W. L. O’Brien and B. P. Tonner, Surface Science 334, 10-18 (1995).

“Room temperature magnetic phases of Fe on fcc Co(001) and Ni(001),” W. L. O’Brien and B. P. Tonner, Phys. Rev. B 52, 15332 (1995).

“Anomalous perpendicular magnetism in Ni/Cu(001) films and the effects of capping layers,” W. L. O’Brien and B. P. Tonner, J. Appl. Phys. 79, 5623-5625 (1996).